## Slide 1
Fast dynamics of glass forming liquids
P. Lunkenheimer, M. Köhler, S. Kastner, and A. Loidl
Center for Electronic Correlations and Magnetism
Experimental Physics V, University of Augsburg, Germany
Broadband dielectric response of glass formers
The fast process of MCT in dielectric spectroscopy
Glycerol with LiCl
Correlation of  and fast process

## Slide 2
  Measurement of dielectric constant and complex conductivity
  Parameters: frequency, temperature (0.1K - 1500K), ac-voltage (<2000V), magnetic field (<14T)
  Extremely broad frequency range: 10-6 Hz <  < 1015 Hz
for details, see U. Schneider, P. Lunkenheimer, A. Pimenov, R. Brand, and A. Loidl, Ferroelectrics 249, 89 (2001)
Experimental Details

## Slide 3
Glassy Dynamics
Broadband dielectric response of dipolar glassforming liquids:
-relaxation – structural relaxation → viscosity
excess wing = slow 
"Johari-Goldstein process"
fast process: cage effect
explained by mode-coupling theory (Götze et al.)
boson peak:
vibrational excitations (?)
intramolecular modes
P. Lunkenheimer and A. Loidl, Contemp. Phys. 41, 15 (2000); Chem. Phys. 284, 205 (2002)

## Slide 4
Glassy Dynamics: Temperature Dependence
P. Lunkenheimer et al., in Structural Glasses and Supercooled Liquids, edited by P.G. Wolynes and V. Lubchenko (Wiley, Hoboken, 2012)

## Slide 5
P. Lunkenheimer et al., PRL 77, 318 (1996); P. Lunkenheimer and A. Loidl, Chem. Phys. 284, 205 (2002); P. Lunkenheimer et al., PRL 95, 055702 (2005)
M. Köhler, P. Lunkenheimer, and A. Loidl, unpublished; M. Köhler, PhD thesis (2010)
U. Schneider et al., Phys. Rev. E 59, 6924 (1999)
Broadband Dielectric Spectra of Glassformers
M. Köhler et al., JNCS 356, 529 (2010); M. Köhler, PhD thesis (2010)

## Slide 6
S. Kastner et al., JNCS 357, 510 (2011)
P. Lunkenheimer et al., PRE 77, 031506 (2008); M. Köhler, PhD thesis (2010)
M. Köhler et al., JNCS 356, 529 (2010); M. Köhler, PhD thesis (2010)
M. Köhler et al., JNCS 356, 529 (2010); M. Köhler, PhD thesis (2010)
Broadband Dielectric Spectra of Glassformers
S. Kastner et al., JNCS 357, 510 (2011)

## Slide 7
The Fast Process in Idealized MCT
Experiment:
Excess intensity in the minimum region between wing/-peak and boson peak
Predicted by mode coupling theory
and ascribed to cage effect
Minimum: sum of two power laws:
a and b correlated:
System parameter : temperature-independent
Critical behavior:
with
U. Bengtzelius, W. Götze, and A. Sjölander, J. Phys. C 17, 5915 (1984); E. Leutheuser, Phys. Rev. A 29, 2765 (1984); W. Götze, Z. Phys. B 60, 195 (1985); W. Götze and L. Sjögren, Rep. Progr. Phys. 55, 241 (1992)

## Slide 8
Conventional scenario: Peak at high   minimum
The Fast Process: A New Scenario
L.C. Pardo, P. Lunkenheimer, and A. Loidl, PRE 76, 030502(R) (2007)
W. Götze, M. Sperl: Fast process leads to Cole-Cole-peak
W. Götze and M. Sperl, Phys. Rev. Lett. 92, 105701 (2004); M. Sperl, Phys. Rev. E 74, 011503 (2006)
New scenario: Peak at low   excess wing!

## Slide 9
The Fast Process in Dielectric Spectroscopy
Minimum in dielectric loss
Excess intensity in minimum region (no trivial superposition!)
MCT fits work over 2-3 frequency decades
P. Lunkenheimer et al., PRL 77, 318 (1996); P. Lunkenheimer et al., PRL 78, 2995 (1997); U. Schneider et al., Phys. Rev. E 59, 6924 (1999)
[Ca(NO3)2]0.4[KNO3]0.6 (CKN)

## Slide 10
M. Köhler et al., JNCS 356, 529 (2010); S. Kastner et al., JNCS 357, 510 (2011); M. Köhler, PhD thesis (2010)
The Fast Process in Dielectric Spectroscopy: Recent Results

## Slide 11
The Fast Process: Critical Laws
P. Lunkenheimer et al., PRL 77, 318 (1996); P. Lunkenheimer et al., PRL 78, 2995 (1997); U. Schneider et al., Phys. Rev. E 59, 6924 (1999)

## Slide 12
The Fast Process: Critical Laws
M. Köhler et al., JNCS 356, 529 (2010); S. Kastner et al., JNCS 357, 510 (2011); M. Köhler, PhD thesis (2010)

## Slide 13
The Fast Process
More sophisticated analyses within mode coupling theory:
"Two-component schematic" mode-coupling model:
Dumbbell molecule in hard-sphere liquid:
W. Götze and Th. Voigtmann, PRE 61, 4133 (2000)
W. Götze, A.P. Singh, and Th. Voigtmann, PRE 61, 6934 (2000)
dielectric spectroscopy
light scattering
propylene carbonate
propylene carbonate
light
scattering
diel. spectr.

## Slide 14
LiCl in Glycerol: Broadband Spectra
M. Köhler, P. Lunkenheimer, and A. Loidl, Eur. Phys. J. E 27, 115 (2008); M. Köhler, P. Lunkenheimer, Y. Goncharov, and A. Loidl, unpublished; M. Köhler, PhD thesis (2010)

## Slide 15
LiCl in Glycerol: Fast Process
LiCl addition  minimum broadens
M. Köhler, P. Lunkenheimer, Y. Goncharov, and A. Loidl, unpublished; M. Köhler, PhD thesis (2010)

## Slide 16
Minimum can be well fitted with MCT interpolation formula
LiCl addition  system parameter  increases
M. Köhler, P. Lunkenheimer, Y. Goncharov, and A. Loidl, unpublished; M. Köhler, PhD thesis (2010)
LiCl in Glycerol: Fast Process

## Slide 17
LiCl in Glycerol: Fast Process
MCT parameters
Minimum broadening with LiCl addition
 Decrease of a and b (increase of )
 Variation in temperature dependence of  peak via:
and
M. Köhler, P. Lunkenheimer, Y. Goncharov, and A. Loidl, unpublished; M. Köhler, PhD thesis (2010)

## Slide 18
P. Lunkenheimer et al., PRL 77, 318 (1996); M. Köhler, PhD thesis (2010)
LiCl in Glycerol: Fast Process
Critical laws and determination of Tc

## Slide 19
LiCl in Glycerol: Correlation  / fast
MCT: 
mol% LiCl | a | b | b/(a+b)
0% | 0.325 | 0.63 | 0.66
4% | 0.322 | 0.62 | 0.66
10% | 0.302 | 0.55 | 0.65
20% | 0.284 | 0.49 | 0.63
M. Köhler et al., unpublished; M. Köhler, PhD thesis (2010)
but:
part of the above data are from below Tc!

## Slide 20
Correlation of  and fast process
glycerol | 0.325 | 0.63 | 0.66
gly/4% LiCl | 0.322 | 0.62 | 0.66
gly/10% LiCl | 0.302 | 0.55 | 0.65
gly/20% LiCl | 0.284 | 0.49 | 0.63
PC | 0.29 | 0.5 | 0.63
PG | 0.33 | 0.653 | 0.66
DPG | 0.319 | 0.612 | 0.66
TPG | 0.302 | 0.55 | 0.65
sorbitol | 0.283 | 0.49 | 0.63
xylitol | 0.297 | 0.53 | 0.64
Salol | 0.352 | 0.75 | 0.68
CKN | 0.3 | 0.54 | 0.64
CRN | 0.2 | 0.28 | 0.58
glycerol | 0.325 | 0.63 | 0.66
gly/4% LiCl | 0.322 | 0.62 | 0.66
gly/10% LiCl | 0.302 | 0.55 | 0.65
gly/20% LiCl | 0.284 | 0.49 | 0.63
PC | 0.29 | 0.5 | 0.63
PG | 0.33 | 0.653 | 0.66
DPG | 0.319 | 0.612 | 0.66
TPG | 0.302 | 0.55 | 0.65
sorbitol | 0.283 | 0.49 | 0.63
xylitol | 0.297 | 0.53 | 0.64
Salol | 0.352 | 0.75 | 0.68
CKN | 0.3 | 0.54 | 0.64
CRN | 0.2 | 0.28 | 0.58
P. Lunkenheimer, M. Köhler, S. Kastner, and A. Loidl, unpublished

## Slide 21
Summary
Data on fast process for 14 (structural) glass formers
Reasonable description by idealized MCT (more sophisticated analysis still missing for most materials)
Glycerol with LiCl: Broadening of loss minimum
Correlation of  and fast process - explanation?

## Slide 22
Thank you!